0501_Surface

User name: Phenom-World-PC\Phenom-World

Contains 2 images with a total of 2 analyses

01. With Beam

1 analysis: 1x map

02. Without Beam

1 analysis: 1x map

With Beam

1. map

| Combined map | Element Number; Element Symbol; Element Name; Atomic Conc.; Weight Conc.. 28; Ni K; Nickel; 83.07; 84.70. 24; Cr K; Chromium; 16.93; 15.30. |
| --- | --- |

FOV: 59.7 µm, Mode: 15kV - Map, Detector: BSD Full, Time: JUL 23 2026 13:53

Disabled elements: B, F, La

Overridden shells used for quantification: Cr K, Mn K, Fe K, Ni K, Mo L

Cut out of map (resolution: 256x223 pixels)

| Nickel | Chromium |  |
| --- | --- | --- |

Without Beam

1. map

| Combined map | Element Number; Element Symbol; Element Name; Atomic Conc.; Weight Conc.. 28; Ni K; Nickel; 80.45; 82.28. 24; Cr K; Chromium; 19.55; 17.72. |
| --- | --- |

FOV: 59.7 µm, Mode: 15kV - Map, Detector: BSD Full, Time: JUL 23 2026 14:32

Disabled elements: B, F, La

Overridden shells used for quantification: Cr K, Mn K, Fe K, Ni K, Mo L

Cut out of map (resolution: 256x219 pixels)

| Nickel | Chromium |  |
| --- | --- | --- |