1219_Surface

User name: Phenom-World-PC\Phenom-World

Contains 2 images with a total of 2 analyses

01. With beam

1 analysis: 1x map

02. Without beam

1 analysis: 1x map

With beam

1. map

| Combined map | Element Number; Element Symbol; Element Name; Atomic Conc.; Weight Conc.. 28; Ni K; Nickel; 83.78; 85.36. 24; Cr K; Chromium; 16.22; 14.64. |
| --- | --- |

FOV: 59.7 µm, Mode: 15kV - Map, Detector: BSD Full, Time: JUL 24 2026 10:06

Disabled elements: B, F, La

Overridden shells used for quantification: Cr K, Mn K, Fe K, Ni K, Mo L

Cut out of map (resolution: 250x256 pixels)

| Nickel | Chromium |  |
| --- | --- | --- |

Without beam

1. map

| Combined map | Element Number; Element Symbol; Element Name; Atomic Conc.; Weight Conc.. 28; Ni K; Nickel; 80.88; 82.69. 24; Cr K; Chromium; 19.12; 17.31. |
| --- | --- |

FOV: 59.7 µm, Mode: 15kV - Map, Detector: BSD Full, Time: JUL 24 2026 11:02

Disabled elements: B, F, La

Overridden shells used for quantification: Cr K, Mn K, Fe K, Ni K, Mo L

Cut out of map (resolution: 256x222 pixels)

| Nickel | Chromium |  |
| --- | --- | --- |